MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

CAT 10W Transmission Oil

Midlands Lubricants Cat 10W Transmission Oil is a high quality mono-grade oil designed to meet the requirements of Caterpillar transmissions and drives. Cat 10W is formulated from solvent refined paraffinic base oils and high performance additives to provide excellent frictional characteristic together with high antiwear and extreme pressure performance.

Cat 10W is recommended for a wide range of lubrication applications, such as

powershift and hydrostatic transmissions, final drives and hydraulic systems in

vehicles where Caterpillar TO-4 and/or Allison C4 performance is specified.

Features/Benefits:

Designed for Off-Highway Automatic and Non-Synchronised Manual

Transmissions, Wet Brakes and Axles

Formulated for Optimum Powershift Transmission Performance

Balanced Frictional Characteristics for Minimimal Brake Noise

Good Anti-Wear Performance and Corrosion Protection

High Resistance to Oxidation for Long Life Lubrication

Performance/Specifications:

Cat 10W meets a comprehensive range of international performance and

specification requirements including:

Caterpillar TO-4

Allison C4

Typical Properties:

Density, g.cm-3 @ 15°C 0.878

Flash Point, COC 220°C

Pour Point -38°C

Viscosity

Kinematic, 40°C 28 cSt

Kinematic, 100°C 5 cSt

Viscosity Index 110

These data are typical of current production, and whilst future production will meet these specifications, some variation in typical data may occur.