MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

10w/40 Motorcycle Semi Synthetic Engine Oil – T4 API SL/CF

# Product Description

Midlands Lubricants 10w/40 semi synthetic motorcycle with JASO MA Anti-slip is a specially formulated semi-synthetic engine oil for riders of high performance bikes who push their machines to the limit and demand a high performance oil but, also need ultimate protection and cleanliness. 10w/40 is a synthetic oil which exceeds the highest international specification and OEM motorcycle manufacturers requirements.

FEATURES / BENEFITS

Exceptional thermal stability helping resist oxidisation and high-temperature derogation. Optimise wet clutch performance along with maximum shear stability to help resist viscosity shear. Outstanding protection against engine wear as well as wear of transmission components. Excellent low temperature characteristics to help minimise engine wear during start up.

PERFORMANCE / SPECIFICATIONS

- API: SL/CF

- ACEA: A3, B3, B4

- JASO MA

TYPICAL PROPERTIES

- Total Base Number (TBN) 10 mgKOH/g

- Specific Gravity, 15°C 0.884 g/cm3

- Flash Point, COC 214 °C

- Viscosity Kinematic, 40°C 96 cSt

- Kinematic, 100°C 14.8 cSt

- Viscosity Index 139

- Pour Point -30°C