MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Pro Cut 22 FSAM

Chlorine free neat cutting oil

Midlands Lubricants Pro Cut 22 FSAM is a chlorine free neat cutting oil developed for use on ferrous materials across a wide range of machinery. Typical applications include general machining on bar autos and automatic machines, drilling, deep hole boring, thread cutting and broaching.

Midlands Lubricants Pro Cut 22 FSAM combines specially selected high performance additives - inactive sulphur EP, lubricity, antimist and anti- oxidant making it suitable for use on all types of ferrous materials.

| Pro Cut 22 FSAM is a low viscosity product and is an excellent choice for use on CNC sliding head lathes where manufacturers require a flexible option for high performance machining with good lubrication minimum product drag out. The products low viscosity ensures rapid penetration to the cutting tool / work piece zone to provide maximum flushing of swarf and chippings. Application & Benefits  Broaching  Thread Cutting  Deep hole drilling and boring  Turning  Milling  Centreless grinding  Rolling and forming  Excellent performance characteristics  Contains inactive Sulphur EP  Contains Anti-mist additive  Anti oxidant formulation to maximise oil life  Formulated on high quality mineral oil  Light Colour  Excellent finish properties  Can be recycled using our recovery service Directions for use |
| --- |
| Shelf life 3 years from date of manufacture |
| Designed to be used as supplied and is safe to use on most metals. |
| Store sealed in a cool dry place between 5°C and 30°C material should always be stored indoors and protected from extremes of temperature. |
| For guidance on handling and disposal please refer to the Material Safety Data Sheet |
| Pro Cut 22 FSAM |
| Characteristics | Typical Data | Characteristics | Typical Data |
| Appearance | Amber | Chlorine | No |
| Viscosity @40oC | 22 cst | Ester | Yes |
| Specific Gravity | 0.875 | Sulphur | Yes |