MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Gear Compound Oils

Product Description

Midlands Lubricants provides a comprehensive range of high quality extreme pressure industrial gear oils meeting the requirements of major reduction gear manufacturer. Formulated from high viscosity index solvent refined mineral base oils, and incorporating additives that provide protection against extreme pressure, wear, corrosion, oxidation and foaming.

Gear Compound oils are used in heavy enclosed industrial gear drives containing spur, helical and bevel gears as well as spiral bevel and worm gears including those operating at high speeds or very high loads. They can also be used for chain drives, sprockets, plain and anti-friction bearings, guideways, flexible couplings, etc. In industrial plants where service conditions require the use of an EP gear lubricant, it meets the severe requirements of all gear drives, including those of steel rolling mills, cement mill gears, cranes and mining equipment.

Features/Benefits:

 High Film Strength with Excellent Load Carrying Capacity

 Good Anti-wear Properties

 Protection Against Shock Load

 Excellent Thermal and Oxidative Stability

 Good Hydrolytic Stability and Water Separation / Demulsibility

 Good Anti-Foam and Air Release Characteristics

 Protection against Rust and Corrosion

 High Viscosity Index and Low Pour Point

 Rubber Compatible

 Prolonged Equipment Life

Performance/Specifications:

 ISO: 12925-1 type CKD

 DIN: 51517 Pt 3 (CLP)

 AGMA: 9005 – EO2

 US Steel: 224

 David Brown: S1.53.101

| Typical Properties: Gear Compound | 68 | 100 | 150 | 220 | 320 | 460 |
| --- | --- | --- | --- | --- | --- | --- |
| Density, g.ml-1 | 0.899 | 0.894 | 0.898 | 0.901 | 0.903 | 0.910 |
| Kinematic Viscosity |  |  |  |  |  |  |
| at 40°C, cSt | 68 | 100 | 150 | 220 | 320 | 460 |
| at 100°C, cSt | 9 | 11 | 15 | 19 | 24 | 31 |
| Viscosity Index | 107 | 99 | 98 | 98 | 98 | 97 |
| Pour Point, °C | -27 | -24 | -21 | -21 | -18 | -10 |
| Flash Point, COC, °C | 230 | 240 | 240 | 245 | 250 | 260 |