MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Hydraulic Jack Oil ISO VG 32

Product Description

Hydraulic Jack Oil is a clear, viscous, refined petroleum liquid for protecting and lubricating hydraulic units. Hydraulic Jack Oil is specially designed to lubricate, prevent sludge formation and resist rusting in hydraulic units. It preserves seals and is non-foaming. It maintains correct viscosity and permits hydraulic actuating mechanisms to function properly. Hydraulic Jack Oil contains antioxidant, anti-rust and anti-wear additives for maximum service life. It is non-corrosive to steel, aluminium alloy, magnesium, plated steel, cadmium and copper.

Features/Benefits:

 Excellent anti-wear, anti-corrosion, anti-rust performance

 Low air retention / air entrainment

 Low foaming

 Shear stable

 Good thermal stability and resistance to oxidation

Performance/Specifications:

Hydraulic Jack oil meets a comprehensive range of international performance and specification requirements including:

 DIN 51524, Part 2 (HLP)

 ISO 6743/4, Type: HM

 Vickers: I-286-S

| Typical Properties: Density, g.cm-3 @ 15.5°C | 0.870 |
| --- | --- |
| Flash Point, COC | 216°C |
| Pour Point | -30°C |
| Viscosity |  |
| Kinematic, 40°C | 32 cSt |
| Kinematic, 100°C | 5.2 cSt |
| Viscosity Index | 102 |