MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Hydraulic Oils

Product Description

Midlands Lubricants provides a comprehensive range of premium quality hydraulic oils formulated from high viscosity index solvent refined mineral base oils with additives to provide excellent protection against oxidation, corrosion, wear and foaming.

ISO viscosity grades 220, 320.

 DIN 51524, Part 2 (HLP) ISO 6743/4, Type: HM Vickers: I-286-S

| Typical Properties ISO Grade |  | 5 |  |  | 10 |  | 15 |  | 22 |  | 32 |  |  | 46 |  | 68 | 100 | 150 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Type |  | HM |  |  | HM |  | HM |  | HM |  | HM |  |  | HM |  | HM | HM | HM |
| Kinematic Viscosity |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ...at 0°C, cSt |  |  | 21 |  | 60 |  | 110 |  | 195 |  | 300 |  |  | 550 |  | 925 | 1730 | 3000 |
| ...at 20°C, cSt |  |  | 9.5 |  | 21.5 |  | 35 |  | 55 |  | 80 |  |  | 130 |  | 200 | 340 | 550 |
| at 40°C, cSt |  |  | 5.0 |  | 10 |  | 15 |  | 22 |  | 32 |  |  | 46 |  | 68 | 100 | 150 |
| at 100°C, cSt |  |  | -- |  | 2.5 |  | 3.3 |  | 4.2 |  | 5.2 |  |  | 6.7 |  | 8.6 | 11.2 | 16.0 |
| Viscosity Index |  |  | -- |  | 80 |  | 84 |  | 90 |  | 102 |  |  | 100 |  | 100 | 100 | 101 |
| Flash Point, COC, °C |  |  | 65 |  | 162 |  | 174 |  | 192 |  | 216 |  |  | 220 |  | 232 | 240 | 267 |
| Pour Point, °C |  |  | -48 |  | -45 |  | -33 |  | -30 |  | -30 |  |  | -30 |  | -28 | -24 | -24 |
| Density, g.ml-1 |  |  | 0.84 |  | 0.86 |  | 0.87 |  | 0.87 |  | 0.87 |  |  | 0.87 |  | 0.88 | 0.88 | 0.89 |
| ASTM D943: 1000 hr TOST, TAN |  |  |  |  |  |  |  |  |  |  |  | Less than 2.0 mgKOH.g-1 |  |  |  |  |  |  |
| IP154: Copper Corrosion |  |  |  |  |  |  |  |  |  |  |  | PASS - Rating 1 |  |  |  |  |  |  |
| DIN 51389: Vickers Vane Pump, Wt Loss |  |  |  |  |  |  |  |  |  |  |  | Less than 50 mg |  |  |  |  |  |  |
| ASTM D1401: Demulse, mins |  |  |  | 3 |  | 7 |  | 8 |  | 9 |  |  | 9 |  | 12 | 21 | 25 | 36 |
| IP 153B: Salt Water Corrosion |  |  |  | Pass |  | Pass |  | Pass |  | Pass |  |  | Pass |  | Pass | Pass | Pass | Pass |
| IP 313: ARV 50°C, 0.2% air |  |  |  | 2 |  | 3 |  | 4 |  | 5 |  |  | 6 |  | 7 | 9 | 12 | 14 |
| IP 146: Foaming Tendency / Stability |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Sequence I | 10/0 |  |  |  | 10/0 |  | 15/0 |  | 15/0 |  | 20/0 |  |  | 30/0 |  | 40/0 | 40/0 | 40/0 |
| Sequence II | 5/0 |  |  |  | 5/0 |  | 10/0 |  | 10/0 |  | 10/0 |  |  | 10/0 |  | 10/0 | 40/0 | 40/0 |
| Sequence III | 10/0 |  |  |  | 10/0 |  | 15/0 |  | 15/0 |  | 20/0 |  |  | 20/0 |  | 40/0 | 40/0 | 40/0 |
| IP 278: Seal Compatibility | 17.5 |  |  |  | 16.5 |  | 14.5 |  | 13.5 |  | 10.6 |  |  | 9.5 |  | 7.5 | 5.0 | 2.5 |