MIDLANDS LUBRICANTS LTD.

Technical Data

PRODUCT NAME :  RED LITHIUM COMPLEX 2                      PRODUCT CODE : 0256/0594

A specially developed multi-purpose lithium complex grease for lubricating all anti-friction and plain bearings for use in industrial and automotive applications. The grease has shown exceptional performance providing extended lubrication intervals over wide operating temperature range.

FEATURES

- Exceptional mechanical stability extends relubrication intervals

- Excellent oxidation stability provides lasting lubrication at high temperatures

- Excellent EP and anti-wear performance

- Good corrosion resistance protects components operating in wet conditions

METHOD OF APPLICATION

RED LITHIUM COMPLEX 2 can be applied manually, or by using a standard grease gun (400gm cartridges available), or via a central lubricating system designed for and capable of pumping an NLGI No.2 grease; consult a qualified centralised lubrication systems engineer before installation.

As with all greases used for the first time, check compatibility with the grease applied previously and if necessary purge bearings prior to application. Likewise, as a general rule, take care not to over-lubricate and apply the quantity of grease recommended by the bearing manufacturer.

| Properties | Specification | Results |
| --- | --- | --- |
| Appearance | - | Smooth grease |
| Colour | - | Red |
| NLGI classification | - | 2 |
| Thickener | - | Lithium complex |
| Base oil | - | Refined mineral oil |
| Worked penetration | IP50 | 265-295 |
| Dropping point (C) | IP132 | 250 min |
| Oil separation (%) | IP121 | 5 max |
| Copper corrosion | IP112 | Pass |
| Resistance to corrosion Emcor (a) | IP 220 | 0:0 |
| Water washout @ 39C % | ASTM D1264 | 3 |
| Four Ball Weld Load (kgs) | IP 239 | 450 |
| Operating temperature range | - | -20ºC to 150ºC |

The information above is believed to be accurate and given in good faith but without warranty. It is  the  users  responsibility to determine the suitability of the product. (Feb 2016)