MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Universal Anti-Freeze

Product Description

Midlands Lubricants Mono Ethylene Glycol Universal Anti-Freeze including organic acid technology inhibitors protects engines against frost damage at temperatures down to -36°C (at 1:1 water dilution ratio). It delivers high protection against rust and corrosion and is suitable for use in the engine coolant system throughout the year.

Features/Benefits:

British Standard BS 6580:1992

Excellent Frost Protection down to -36°C

Provides Protection against Over-Heating

Excellent Corrosion and Rust Protection

Suitable for Constant (All Year) Use

Non-Foaming

Physical Characteristics:

Appearance Blue

Density, g.cm-3 @ 20°C 1.125

Boiling Point (undiluted) 160°C

Reserve Alkalinity (0.1M HCl) 20 ml

pH Value @ 50% aqueous 7.5

Freezing Point, Undiluted -13°C

Freezing Point, 25% aqueous, (1:3)* -16°C

Freezing Point, 33% aqueous, (1:2)* -19°C

Freezing Point, 40% aqueous, (1:1.5)* -24°C

Freezing Point, 50% aqueous, (1:1)* -36°C

Hard Water Compatibility Pass

* Ratio is parts Antifreeze to parts Water

These data are typical of current production, and whilst future production will meet these specifications, some variation in typical data may occur.