MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

10W/40 CJ-4 Engine Oil

Product Description:

Midlands Lubricants 10W/40 CJ4 is a high performance multi-grade low SAPs engine oil incorporating advanced additive technology in superior synthetic base stock. 10W/40 CJ4 designed for the very latest Euro VI engines.

Features/Benefits:

Good high and low temperature performance

Good protection against ring sticking at high temperatures, maintaining

oil performance whilst minimising oil consumption and emissions

Very high standard of engine cleanliness

Excellent sludge control protection

Long lasting dispersant, anti-wear and corrosion protection

Performance/Specifications:

10W/40 CJ-4 engine oil meets the performance requirements of:

API: CJ-4

ACEA: E4-12, E6-12, E7-12, E9-12

MB: 228.31, 228.51

VOLVO – VDS-4

RVI RLD-3/RLD-2, MACK EO-O / EO-N

Ditroit Diesel 93K218

Voith Class B / MB 235.28

Caterpillar: ECF-3

MAN M3477/M3575/M3271-1 MTU type 3.1/2.1

Sciania Low ash

Cummins CES 20081

JASO DH-2

Typical Properties:

Total Base Number (TBN) 12.5 mgKOH.g-1

Density, g.cm-3 @ 15.5°C 0.877

Flash Point, COC 204°C

Pour Point -40°C

Viscosity

Kinematic, 40°C 87 cSt

Kinematic, 100°C 14.7 cSt

Viscosity Index 177