MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Super Universal Tractor Oil 15W/30 SL/CG-4

Product Description

Super Universal Tractor Oil (SUTO) is a high quality/high performance engine oil that meets all the lubrication requirements of farm tractors and agricultural machinery. SUTO is a multi-grade viscosity oil that spans a wide temperature range and is suitable for use in a variety of engines including naturally aspirated and turbocharged diesel and petrol engines. It is suitable for use in tractor hydraulic, transmission, and wet brake systems as well as gear boxes in all farm machinery.

SUTO provides excellent protection under the most arduous operating conditions and is formulated according to the most demanding performance requirements. SUTO includes friction modifier additives to provide smooth operation of the wet brake system to prevent squawk and chatter. SUTO offers the convenience of a single lubricant approach that delivers top performance and avoids the need for stocking of multiple lubricants eliminating the risk of incorrect use in the field.

| Features/Benefits: | Performance/Specifications: |
| --- | --- |
| - ExcellentThermal Stability | SUTO 15W/30 meetsthe followingspecifications: |
| - Reduced Fuel Consumption | - API SL/CG-4 |
| - Low Drag Formulation | - MIL-L-2104C/D, MIL-L-45199B |
| - Reduced Friction | - Caterpillar Series 3 |
| - Rapid Circulation on Start-up | - Ford ESN-86A/B, |
| - Excellent Anti-wearProtection | - Ford M2C 159B |
| - Reduces Oil Inventory | - Ford M2C 134D |
| - Lower Emissions | - John Deere: JD 303, JD 20A, J20C, J14B |
| - Resists Black Sludge | - Case: MS 1206 |
| - Improved Engine Cleanliness | - Massey-Ferguson: 1139, M1135, M1127A |
| - Low Oil Consumption | - MIL-L-2105 |
| - Low Chlorine Formulation (for safe disposal or recycling) | - API GL4 - IH B6 |

Typical Properties:

| TBN | 10.3 mgKOH/g |
| --- | --- |
| Density, g.cm-3@ 15°C | 0.893 |
| Flash Point, COC | 220°C |
| Pour Point | -30°C |
| Sulphated Ash | 1.17% |
| Viscosity |  |
| Kinematic, 40°C | 86cSt |
| Kinematic, 100°C | 11.2cSt |
| Viscosity Index | 128 |