MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

CAT 30W Transmission Oil

Midlands Lubricants Ltd Cat 30W Transmission Oil is a high quality mono-grade oil designed to meet the requirements of Caterpillar transmissions and drives. Cat 30W is formulated from solvent refined paraffinic base oils and high performance additives to provide excellent frictional characteristic together with high antiwear and extreme pressure performance.

Cat 30W is recommended for a wide range of lubrication applications, such as

powershift and hydrostatic transmissions, final drives and hydraulic systems in

vehicles where Caterpillar TO-4 and/or Allison C4 performance is specified.

Features/Benefits:

Excellent Frictional Characteristics for Optimum Powershift

Transmission Performance

Good Anti-Wear and Corrosion Protection

High Resistance to Oxidation for Long Life Lubrication

Performance/Specifications:

Cat 30W meets a comprehensive range of international performance and

specification requirements including:

Caterpillar TO-4

Allison C4

Typical Properties:

Density, g.cm-3 @ 15°C 0.895

Flash Point, COC 225°C

Pour Point -25°C

Viscosity

Kinematic, 40°C 105 cSt

Kinematic, 100°C 12 cSt

Viscosity Index >90

These data are typical of current production, and whilst future production will meet these specifications, some variation in typical data may occur.