MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

# CAT TO-4 SAE 50

Transmission Oil

Cat TO-4 SAE 50 Transmission Oil is a high quality mono-grade oil designed

to meet the requirements of Caterpillar TO-4 and Allison C-4 transmissions

and drives. Cat TO-4 SAE 50 is formulated from solvent refined paraffinic

base oils and high performance additives to provide excellent frictional

characteristic together with high anti-wear and extreme pressure

performance.

Cat TO-4 SAE 50 is recommended for a wide range of lubrication applications,

such as powershift and hydrostatic transmissions, final drives and hydraulic

systems in vehicles where Caterpillar TO-4 and/or Allison C4 performance is

specified.

Features/Benefits:

Excellent Frictional Characteristics for Optimum Powershift

Transmission Performance

Good Anti-Wear and Corrosion Protection

High Resistance to Oxidation for Long Life Lubrication

Performance/Specifications:

Cat TO-4 SAE 50 meets a comprehensive range of international performance

and specification requirements including:

Caterpillar TO-4

Allison C4

Typical Properties:

Density, g.cm-3 @ 15°C 0.890

Flash Point, COC 230°C

Pour Point -20°C

Viscosity

Kinematic, 40°C 220 cSt

Kinematic, 100°C 19 cSt

Viscosity Index >95

These data are typical of current production, and whilst future production will meet these specifications, some variation in typical data may occur