MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

2-Stroke Motor Oil

Product Description

Midlands Lubricants 2-Stroke Motor Oil is a traditional mineral oil based motor oil suitable for use in air and water cooled 2-stroke cycle engines typically used in motorcycles, scooters, mopeds, lawnmowers and horticultural equipment. 2-Stroke Motor Oil is formulated from top quality solvent refined mineral base oils with additive technology designed to deliver optimum performance, and is dyed blue so that its presence in the petrol mixture is readily apparent.

Recommendations:

Under normal running conditions Midlands Lubricants 2-Stroke Motor Oil is

recommended for use at between 16:1 to 24:1 parts petrol:oil, or as

otherwise recommended by the engine manufacturer.

Features/Benefits:

Good Deposit Control

Good Anti-Sludge and Varnish Resistance

Excellent Anti-Wear, Oxidation Stability and Corrosion Protection

Dispersant/Detergent Properties

Resistance to High Sulphur Fuels

Performance/Specifications:

Midlands Lubricants 2-Stroke Motor Oil meets a comprehensive range of international performance and specification requirements including:

API: TC

MIL-L-2104B

JASO FB

Typical Properties:

Appearance Blue

Density, g.cm-3 @ 15°C 0.890

Flash Point, COC 240°C

Viscosity

Kinematic, 40°C 74 cSt

Kinematic, 100°C 10.3 cSt

Viscosity Index 98

These data are typical of current production, and whilst future production will meet these specifications, some variation in typical data may occur.