MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Semi Synthetic 2-Stroke Oil

Product Description

Midlands Lubricants Semi Synthetic 2-Stroke Motor Oil is an advanced 2-stroke oil specifically formulated for use in higher RPM machinery, for example scooters Chainsaws, High-Speed Strimmers, Pumps, Mowers, etc. Semi Synthetic 2-Stroke Oil is formulated from top quality solvent refined mineral base oils with high performance synthetic component additive technology designed to deliver optimum performance, and is dyed red so that its presence in the petrol mixture is readily apparent.

Recommendations:

Under normal running conditions Semi Synthetic 2-Stroke Oil is suitable for

use at ratios as low as 50:1 parts petrol:oil, or can be used at different ratios

as recommended by the equipment manufacturer.

Features/Benefits:

Excellent Detergency

Strong Resistance to Spark Plug Fouling

Reduced Piston Crown and Exhaust Port Deposits

Outstanding Protection Against Rust

Performance/Specifications:

Midlands Lubricants 2-Stroke Motor Oil meets a comprehensive range of international performance and specification requirements including:

API: TC

JASO FC

Typical Properties:

Appearance Red

Density, g.cm-3 @ 15°C 0.906

Flash Point, COC 200°C

Pour Point -20°C

Viscosity

Kinematic, 40°C 90 cSt

Kinematic, 100°C 15.0 cSt

Viscosity Index 98

These data are typical of current production, and whilst future production will meet these specifications, some variation in typical data may occur.