MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

ATF Dexron II

Automatic Transmission and Power Steering Fluid

Product Description

ATF Dexron II is a high performance multi-application fluid meeting General

Motors 6137-M Dexron II and Allison C3 specifications, and is also suitable for

Ford transmissions with a red filler cap. The high viscosity index and low pour

point makes this product ideal for use in hydraulic systems, power steering

and torque converters.

Features/Benefits:

Good friction control

High oxidation and thermal stability

Consistent gear change performance

Excellent fluidity at sub-zero temperatures

Smooth power transmission in all working conditions

Multi-applications: transmissions, torque converters, power steering,

and general hydraulic systems

Performance/Specifications:

ATF Dexron II meets the performance requirements of:

Chrysler MS-6704A

Ford ESP-M2C 138CJ, 166H

Ford Mercon / M2C924-4

GM Dexron IID

MAN 339 Type Z1

MB-Approval 236.5 / 236.6 / 236.7

Typical Properties:

Density, g.ml-3 @ 15°C 0.869

Flash Point, COC, 210°C

Pour Point -36°C

Viscosity

Kinematic @ 40°C 42.5 cSt

Kinematic @ 100°C 8.3 cSt

Viscosity Index 163

These data are typical of current production, and whilst future production will meet these specifications, some variation in typical data may occur.