MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

ATF Dexron III

Automatic Transmission and Power Steering Fluid

Product Description

ATF Dexron III is a premium multifunctional fully formulated automatic

transmission fluid for use in all automatic and powershift transmissions as well

as industrial mobile hydraulic systems.

Features/Benefits:

 Low Temperature Fluidity

 Increased Fuel Economy – Reducing Friction Losses

 Improved Protection for Continuous High Temperature Operation

 Reduced Harmful Deposits

 High Chemical and Thermal Stability

 Gold Seal Compatibility

 Anti-Foam Protection

Performance/Specifications:

ATF Dexron III meets the performance requirements of:

 GM Dexron III

 Ford Mercon

 Mercedes-Benz

 ZF

 Renk

 Voith

 Allison C4

 Caterpillar TO-2

 Hydraulic Pump Systems: Sperry-Vickers, Sunstrand and Denison

Typical Properties:

Density, g.ml-3 @ 15°C 0.858

Flash Point, COC, 210°C

Pour Point -36°C

Viscosity

Kinematic @ 100°C 7.5 cSt

These data are typical of current production, and whilst future production will meet these specifications, some variation in typical data may occur.