MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

80W/90 Gear Oil GL4

Product Description

Midlands Lubricants 80W/90 Gear Oil GL4 is an extreme pressure multi-grade gear oil with anti-scuff properties suitable for axles with spiral bevel gears operating under moderate to severe speed and load conditions. Suitable for use in selected manual transmissions and transaxle applications where API MT-1 lubricants are unsuitable.

Specifications:  API GL4  ZF TE-ML 02A  Volvo 97313  MAN 341

Features/Benefits:

 Extended Gear Box and Axle Life

 Excellent Shock Load Performance

 High Anti-Scuff Protection

 Low Temperature Fluidity

 Non-Corrosive Extreme Pressure Performance

 Low Foam

| Typical Physical Properties: Density, g/cm3 @ 15.5°C (60°F) | 0.885 |
| --- | --- |
| Flash Point, COC | 230°C |
| Pour Point, COC | -15°C |
| Viscosity |  |
| Kinematic, 40°C | 150 cSt |
| Kinematic, 100°C | 14.5 cSt |
| Viscosity Index | 95 |