MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

80W/90 Gear Oil GL5

Product Description

Midlands Lubricants 80W/90 Gear Oil GL5 is a high performance extreme pressure multigrade

gear oil with high anti-scuff properties, meeting the most severe

demands of hypoid final drive gears. Suitable for use in all spiral bevel axles

steering gearboxes where API GL5 and MIL-L-2105D performance is required.

Specifications:

API GL5

MIL-L-2105D

David Brown ET19

Mack GO-G

Ford M2C9002A

GM 4655

VW 727

BLS OL 03

Fiat W90M

Volvo 97313, 97310

MAN 341, 342

Features/Benefits:

Extended Gear Box and Axle Life

Excellent Shock Load Performance

High Anti-Scuff Protection

Low Temperature Fluidity

Non-Corrosive Extreme Pressure Performance

Low Foam

Typical Physical Properties:

Density, g/cm3 @ 15.5°C (60°F) 0.885

Flash Point, COC 230°C

Pour Point, COC -15°C

Viscosity

Kinematic, 40°C 150 cSt

Kinematic, 100°C 14.5 cSt

Viscosity Index 95

These characteristics are typical of current production material, whilst further production will

meet these specifications, some variation may occur.