MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Biodegradable Hydraulic Oil 32

Product Description

Midlands Lubricants Biodegradable Hydraulic Oil 32 is a vegetable oil based lubricant which is an environmentally acceptable alternative to conventional mineral oil based hydraulic fluids. Biodegradable Hydraulic Oil 32 is particularly recommended for use in agriculture and forestry applications and is especially suitable for use where special care for the environment is required such as those applications where there is a risk of loss or spillage to the environment. Biodegradable Hydraulic Oil 32 is formulated with an antifoaming agent to prevent undue foaming in service.

Features/Benefits:

Corrosion Protection, DIN 51585A A-0

CEC L-33-T-82 Biodegradability, > 90%

Formulated to minimise foaming in service

Typical Properties:

Density, g/cm3 @ 15.6°C 0.920

Flash Point, COC 305°C

Pour Point -24°C

Biodegradability, CEC L-33-T-82 > 90%

Viscosity

Kinematic, @ 40°C 32 cSt

Kinematic, @ 100°C 5.4 cSt

Data are typical of current production, and whilst future production will meet these specifications, some batch to batch variation in typical data may occur.