MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Biodegradable Hydraulic

Oil 46

Product Description:

Midlands Lubricants Biodegradable Hydraulic Oil 46 is a vegetable oil based lubricant which is an environmentally acceptable alternative to conventional mineral oil based hydraulic fluids.

Biodegradable Hydraulic Oil 46 is recommended for use in agriculture and

forestry applications and is especially suitable for use where special care for

the environment is required such as those applications where there is a risk of

loss or spillage to the environment.

Biodegradable Hydraulic Oil 46 is formulated with an anti-foaming agent to

prevent undue foaming in service.

Features/Benefits:

Corrosion Protection, DIN 51585A A-0

CEC L-33-T-82 Biodegradability, > 90%

Formulated to minimise foaming in service

Ideal for environmental applications where losses may occur

Typical Properties:

Density, 15.6°C 0.920 g/cm3

Flash Point, COC 320°C

Pour Point -24°C

Biodegradability, CEC L-33-T-82 > 90%

Viscosity

Kinematic, @ 40°C 46 cSt

Kinematic, @ 100°C 8.6 cSt

Viscosity Index 168

Data are typical of current production, and whilst future production will meet these specifications, some batch to batch variation in typical data may occur.