MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

EXLC5 Anti-Freeze

Extended Life

Product Description

Midlands Lubricants Mono Ethylene Glycol Extended life antifreeze product uses inhibitors employing organic acid technology (OAT) to provide long lasting corrosion protection for up to 5 years or 150 000 miles.

Features/Benefits:

Exceeds British Standard BS 6580:2010 and ASTM D3306 type 1 and

exceeds the requirements for most motor manufacturers.

Excellent Frost Protection down to -36°C

Borate/phosphate/nitrite/amine free

Excellent Corrosion and Rust Protection

Non phosphate/ non silicate formulation reduces damage from hard

water

Suitable for Constant (All Year) Use

Non-Foaming

Physical Characteristics:

Appearance Red

Density, g.cm-3 @ 20°C 1.125

Boiling Point (undiluted) 160°C

Reserve Alkalinity (0.1M HCl) 5 ml

pH Value @ 50% aqueous 7.5

Freezing Point, Undiluted -13°C

Freezing Point, 25% aqueous, (1:3)* -16°C

Freezing Point, 33% aqueous, (1:2)* -19°C

Freezing Point, 40% aqueous, (1:1.5)* -24°C

Freezing Point, 50% aqueous, (1:1)* -36°C

Hard Water Compatibility Pass

* Ratio is parts Antifreeze to parts Water

These data are typical of current production, and whilst future production will meet these specifications, some variation in typical data may occur.