MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Universal Transmission Oil

Product Description

Universal Transmission Oil is formulated for use in the transmission and

hydraulic systems of Universals and some commercial plant vehicles with wet

brake systems.

Features/Benefits:

Reduces Brake Chatter and Squawk

Provides High Gear Wear Protection

Enhances Hydraulic Operation

Designed for Universal Applications

Performance/Specifications:

Universal Transmission Oil meets a comprehensive range of international

performance and specification requirements including:

Case: MS 1204, MS 1205, MS 1206, MS 1207, MS 1210

John Deere: JD20A, JD20B, JD20C

Ford: M2C134A-D, M2C41B-48B, M2C53A

Massey-Ferguson: M1135, M1141, M1110, M1127, M1129A,

API: GL4

Allison: C-3, C-4

Caterpillar: TO-2

ZF: TE ML 05, 06

Sperry Vickers: 1-286-S-M2950S

Denison: HF-0, HF-1, HF-2

Typical Properties:

Density, g.cm-3 @ 15°C 0.892

Flash Point, COC 220°C

Pour Point -30,°C

Viscosity

Kinematic, 40°C 45.7 cSt

Kinematic, 100°C 9.2 cSt

Viscosity Index 147

These data are typical of current production, and whilst future production will meet these specifications, some variation in typical data may occur.