MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Fully Synthetic 0W/20 Engine Oil

Product Description

Fully Synthetic 0W/20 is a multigrade engine oil based on synthetic base stocks and

formulated with the very latest in advanced technology, producing a super high

performance engine oil which delivers excellent fuel economy.

Fully Synthetic 0W/20 has been developed to provide outstanding lubrication

performance in up-to-date multi-valve power units which, due to their advanced

design, require the use of lower viscosity multigrade engine oils whilst also providing

improved film strength and oxidation stability.

Specification & Performance Requirements:

Fully Synthetic 0W/20 meets or exceeds the requirements of:

API SN/CF

ACEA A5-12/B5-12

Ilsac GF5

Dexos 1

GM 4718M

Features/Benefits:

Effective fuel efficiency

Excellent high and low temperature performance

Exceptional long term anti-wear characteristics

Very high standard of engine cleanliness

Long lasting dispersant performance and corrosion protection

Excellent sludge control for stop-go city motoring

High temperature protection against ring sticking, ensuring oil performance

and reduced oil consumption and low emissions

Typical Physical Properties:

Total Base Number 8

Density, g/cm3 @ 15.6°C 0.855

Flash Point, COC 220 °C

Viscosity

Kinematic, cSt @ 40°C 38

Kinematic, cSt @ 100°C 8.1

Viscosity Index 168

Cold Crank, -35°C 5500 cP