MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Fully Synthetic 5W/30 Engine Oil

Product Description

5W/30 Fully Synthetic Motor Oil is a super multi-grade engine oil produced

from high quality synthetic base oils incorporating the latest additive

technology to produce a super high performance engine oil that delivers

excellent performance as well as good fuel economy.

Features/Benefits:

Excellent Fuel Efficiency and Sludge Control for Stop-Go City Motoring

Excellent High and Low Temperature Performance

Exceptional Long Term Anti-Wear Characteristics

Very High Standard of Engine Cleanliness

Long-lasting Dispersant Performance and Corrosion Protection

Protects against Ring Sticking at High Temperatures

Reduced Oil Consumption and Emissions

Performance / Specifications:

5W/30 FS meets the performance requirements of the following:

API: SL/CF

ACEA: A1-12/B1-12

ILSAC- GF-3

BMW LL-98

Ford: WSS-MC2 913A, WSS-MC2 913B

Typical Properties:

Density, g/cm3 @ 15°C 0.880

Flash Point, COC 208°C

Pour Point -40°C

Viscosity

Kinematic, @ 40°C 64 cSt

Kinematic, @ 100°C 10.8 cSt

Viscosity Index 137

These data are typical of current production, and whilst future production will meet these specifications, some

variation in typical data may occur.