MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Chain Saw Oil 220

Product Description

Chain Saw Oil is a high quality high viscosity anti-fling lubricating oil produced

from solvent refined base stocks formulated with advanced non-throw

additive to prevent lubricant loss and promote continuous smooth chain

motion for high speed chainsaws.

Features/Benefits:

Advanced non-throw performance

Multi-use chain lubricant

Economical

Reduced Friction

Typical Properties:

Density, g/cm3 @ 15.6°C (60°F) 0.884

Flash Point, COC, °C (°F) 224 (435)

Pour Point, COC, °C (°F) -24 (-11)

Viscosity

Kinematic, cSt @ 40°C 220

Kinematic, cSt @ 100°C 16.5

Viscosity Index 105

These data are typical of current production, and whilst future production will meet these specifications, some variation in typical data may occur.