MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

10w/40 Semi Synthetic Engine Oil

# Product Description

Midlands Lubricants 10W/40 is a specially formulated semi-synthetic engine oil meeting stringent European performance specifications for turbo charged and naturally aspirated petrol and diesel engines working under normal and arduous conditions.

FEATURES / BENEFITS

Excellent High and Low Temperature Performance High Temperature Protection against Ring Sticking High Levels of Engine Cleanliness Ensured Oil Performance and Reduced Consumption Improved Fuel Efficiency Long-Lasting Dispersant and Anti-Wear Performance Good Corrosion Protection Low Emissions

PERFORMANCE / SPECIFICATIONS

- API: SL/CF

- ACEA: A3, B3, B4

- VW: 500.00, 505.00

- MB: 227.5, 229.1

TYPICAL PROPERTIES

- Total Base Number (TBN) 10 mgKOH/g

- Specific Gravity, 15°C 0.884 g/cm3

- Flash Point, COC 214 °C

- Viscosity Kinematic, 40°C 98 cSt

- Kinematic, 100°C 14.0 cSt

- Viscosity Index 155

- Pour Point -47°C