MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

5w/20 ECO FE Fully Synthetic Engine Oil

Product Description

Fully Synthetic 5W/20 is a multigrade engine oil based on synthetic base stocks and formulated with the very latest in advanced technology, producing a super high performance engine oil which delivers excellent fuel economy. Fully Synthetic 5W/20 has been developed to provide outstanding lubrication performance in up-to-date multi-valve power units which, due to their advanced design, require the use of lower viscosity multigrade engine oils whilst also providing improved film strength and oxidation stability.

FEATURES / BENEFITS

Effective fuel efficiency Excellent high and low temperature performance Exceptional long term anti-wear characteristics Very high standard of engine cleanliness Long lasting dispersant performance and corrosion protection Excellent sludge control for stop-go city motoring High temperature protection against ring sticking, ensuring oil performance and reduced oil consumption and low emissions

PERFORMANCE / SPECIFICATIONS

- API SN  -           ACEA A5-12/B5-12

- Ilsac GF5 -        Dexos 1

- GM 4718M WSS-M2C948-B WSS-M2C925 – A/B

TYPICAL PROPERTIES

Total Base Number 8

Density, g/cm3 @ 15.6°C 0.855

Flash Point, COC 220°C

Viscosity Kinematic, cSt @ 40°C 39

Kinematic, cSt @ 100°C 8.8

Viscosity Index 168                  Cold Crank, -30°C 4800 cP