MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

5w/30 C1 Fully Synthetic Engine Oil

Product Description

Midlands Lubricants Fully Synthetic 5W/30 C1 engine oil is produced from high quality synthetic base oils and top-tier performance additives.

FEATURES / BENEFITS

- Suitable for use in petrol and diesel engines requiring the latest Ford and Mazda specified lubricant performance. Blended to ensure fuel efficiency, reduced wear and low emissions.

- Low SAPS technology delivers a high level of engine cleanliness and protection from combustion contamination.

- Provides optimum performance and engine protection at temperature extremes and under high performance conditions.

PERFORMANCE / SPECIFICATIONS

ACEA: C1-12

JASO DL-1

FORD – WSS M2C 934-B

TYPICAL PROPERTIES

TBN, mgKOH.g-1 7.2

Density, g/cm3 @ 15°C 0.856

Flash Point, COC 220°C

Pour Point -40°C

Viscosity Kinematic, @ 40°C 62 cSt

Kinematic, @ 100°C 11.9 cSt

Viscosity Index 192