MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

5w/30 C2 – Full Synthetic Engine Oil

Product Description

Midlands Lubricants Fully Synthetic 5W/30 C2 engine oil is produced from high quality synthetic base oils and top-tier performance additives, specially formulated for use in Euro IV compliant vehicles fitted with after treatment devices.

FEATURES / BENEFITS

Suitable for use in Euro IV compliant petrol and diesel engines using after treatment devices Blended to ensure fuel efficiency, excellent wear protection and good sludge control performance Mid SAPS technology delivers a high level of engine cleanliness and protection from combustion contamination. Provides optimum performance and engine protection under high performance conditions and at temperature extremes.

PERFORMANCE / SPECIFICATIONS

- API: SN/CF

- ACEA: C2-12

- Renault RN0700

- PSA B71 2290 (2012)

- Fiat 9.55535-S1

TYPICAL PROPERTIES

- Total Base Number 8

- Density, g/cm3 @ 15°C 0.855

- Flash Point, COC 220°C

- Pour Point -40°C

- Viscosity Kinematic, @ 40°C 60 cSt

- Kinematic, @ 100°C 10 cSt Viscosity Index 153