MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

5w/30 C4 – Full Synthetic Engine Oil

Product Description

Midlands Lubricants Fully Synthetic 5W/30 C4 engine oil is produced from high quality synthetic base oils and top-tier performance additives.

FEATURES / BENEFITS

Suitable for use in petrol and diesel engines requiring the latest Renault specified lubricant performance Blended to ensure fuel efficiency, reduced wear and low emissions. Low SAPS technology delivers a high level of engine cleanliness and protection from combustion contamination. Provides optimum performance and engine protection at temperature extremes and under high performance conditions.

PERFORMANCE / SPECIFICATIONS

- ACEA: C4-12

- MB: 226.51

- Renault RN0720

TYPICAL PROPERTIES

- Total Base Number (TBN) 7.2

- Density, g/cm3 @ 15°C 0.856

- Flash Point, COC 220°C

- Pour Point -40°C

- Viscosity Kinematic, @ 40°C 64 cSt

- Kinematic, @ 100°C 11.7 cSt

- Viscosity Index 189