MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

5w/30 FS 913D Ford Full Synthetic Engine Oil

Product Description

Midlands Lubricants 5W/30 FS 913D is a fully-synthetic high performance motor oil that delivers outstanding performance with high fuel economy and is suitable for use in Ford vehicles requiring Ford M2C 913D specified performance levels.

FEATURES / BENEFITS

Excellent protection against wear throughout the engine

Excellent piston deposit control

Good protection against sludge formation.

PERFORMANCE / SPECIFICATIONS

- API: SN/CF*

- ACEA: A5-12/B5-12

- Ford: M2C 913D / 913C RN 0700

- STJLR 03.5003

TYPICAL PROPERTIES

- Total Base Number 10 mgKOH/g

- Density, g/cm3 @ 15°C 0.860

- Flash Point 210°C

- Pour Point -35°C

- Kinematic Viscosity, 40°C 55 cSt

- Kinematic Viscosity, 100°C 9.5 cSt

- Viscosity Index 157