MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

5w/30 GM Fully Synthetic Engine Oil

Product Description

Midlands Lubricants Fully Synthetic 5w/30 GM is formulated according to the requirements of GM/Vauxhall/Opel petrol and diesel vehicles operating under extended drain intervals. Formulated from high quality synthetic base oils with additive technology especially designed to ensure high cleanliness and prolonged lubricant life it delivers excellent engine performance with reduced emissions and good fuel economy. Fully Synthetic 5w/30 GM provides optimum engine protection even when operating under extreme hot and cold climate conditions, yet maintains maximum performance throughout.

FEATURES / BENEFITS

Suitable for GM/Vauxhall/Opel Petrol and Diesel vehicles operating under extended drain intervals

Excellent High and Low Temperature Performance

Excellent Fuel Efficiency and Sludge Control for Stop-Go City Motoring

Very High Standard of Engine Cleanliness Long-Lasting Performance and Corrosion Protection Reduced Oil Consumption and Emissions

PERFORMANCE / SPECIFICATIONS

- API: SL/CF

- ACEA: A3/B3, A3/B4

- MB: 229.3

- GM: LL-025-A/B

- BMW: Longlife 01 VW: 502.00, 505.00

TYPICAL PROPERTIES

- Density, g/cm3 @ 15°C 0.860

- Flash Point, COC 220°C

- Pour Point -35°C

- Viscosity Kinematic, @ 40°C 61 cSt

- Kinematic, @ 100°C 11.7 cSt

- Viscosity Index 191