MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

5w/30 Semi Synthetic Engine Oil

# Product Description

Midlands Lubricants 5W/30 semi-synthetic engine oil is a unique combination of highly refined mineral and synthetic base oils incorporating high performance engine oil additives to deliver a lubricant with exceptional performance and engine protection. The reduced frictional characteristics of this 5W/30 oil provides a balance of enhanced fuel economy with extra power output.

FEATURES / BENEFITS

Excellent Thermal Stability Low Chlorine Formulation, (for safer and easier disposal or recycling) Improved Fuel Efficiency Suitable for use in Ford Zetec engines Improved Engine Cleanliness Low Oil Consumption and Low Emissions Rapid Circulation on Start-up Reduced Pinking and Combustion Chamber Deposits at Extreme Temperatures, (300°C)

PERFORMANCE / SPECIFICATIONS

- API: SL/CF

- ACEA: A1-12/B1-12,

- Ford: WSS M2C 913-A

- Ford: WSS M2C 913- B

TYPICAL PROPERTIES

- TBN, mgKOH.g-1 9

- Density, g/cm3 @ 15.6°C (60°F) 0.861

- Flash Point, COC 214°C Pour Point -40°C

- Viscosity Kinematic, @ 40°C 58 cSt

- Kinematic, @ 100°C 11 cSt

- Viscosity Index 137