MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

5w/40 API SL Full SAPS - Full Synthetic Engine Oil

Product Description

Midlands Lubricants Fully Synthetic 5W/40 is a super multi-grade engine oil produced from high quality synthetic base oils incorporating the latest additive technology to produce a super high performance engine oil that delivers excellent fuel economy. Fully Synthetic 5W/40 has been developed to provide outstanding performance in the latest multi-valve technology power units requiring lighter viscosity lubricants that must also deliver good protection, film strength and oxidation stability under more demanding operating conditions

FEATURES / BENEFITS

Excellent Fuel Efficiency and Sludge Control for Stop-Go City Motoring Excellent High and Low Temperature Performance Exceptional Long Term Anti-Wear Characteristics Very High Standard of Engine Cleanliness Long-lasting Dispersant Performance and Corrosion Protection Protects against Ring Sticking at High Temperatures Reduced Oil Consumption and Emissions

PERFORMANCE / SPECIFICATIONS

- API: SL/CF

- ACEA: A3-12 B4-12

- MB: 229.3, MB 229.1

- BMW: LL-98

- Porsche A40 VW: 501.00, 502.00, 505.00

TYPICAL PROPERTIES

- Density, g/cm3 @ 15°C 0.854

- Flash Point, COC 208°C

- Pour Point -39°C

- Viscosity Kinematic, @ 40°C 87 cSt

- Kinematic, @ 100°C 14.8 cSt

- Viscosity Index 154