MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

5w/40 PD – Full Synthetic Engine Oil

Product Description

Midlands Lubricants 5W/40 PD 505.01 FS Motor Oil is a fully synthetic engine oil produced from high quality synthetic base oils and high level performance additives, especially formulated for use in VW, Audi, Skoda and Ford vehicles fitted with VW unit injector diesel engines.

FEATURES / BENEFITS

Suitable for use in petrol and diesel engines requiring VW specified 505.01 lubricant performance Blended to ensure fuel efficiency, reduced wear and low emissions. Mid-low SAPS technology delivers a high level of engine cleanliness and protection from combustion contamination. Provides optimum performance and engine protection at temperature extremes and under high performance conditions. Recommended for vehicles 2004-2008 requiring A3,B3,B4

PERFORMANCE / SPECIFICATIONS

- VW: 502/505.01

- ACEA:C3-12

- API: SN/CF

- BMW: LL-04

- MB: 226.5 229.31 229.51

- Porsche A40

- FORD: WSS-M2C917A

- GM Dexos 2

- Renault RN 0700, RN 0710

TYPICAL PROPERTIES

- TBN, mgKOH.g-1 8

- Density, g/cm3 @ 15°C 0.850

- Flash Point, COC 226°C Pour Point -40°C

- Viscosity Kinematic, @ 40°C 95 cSt

- Kinematic, @ 100°C 14.4 cSt

- Viscosity Index 156