MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Chain Saw Oil 150

Product Description

Midlands Lubricants Chain Saw 150 Oil is a high quality high viscosity anti-fling lubricating oil produced from solvent refined base stocks formulated with advanced non-throw additive to prevent lubricant loss and promote continuous smooth chain motion for high speed chainsaws.

# FEATURES / BENEFITS

- Advanced non-throw performance

- Multi-use chain lubricant

- Economical

- Reduced Friction

# TYPICAL PROPERTIES

- Density, g/cm3 @ 15.6°C (60°F) 0.884

- Flash Point, COC, °C (°F) 224 (435)

- Pour Point, COC, °C (°F) -24 (-11)

- Viscosity Kinematic, cSt @ 40°C 150

- Kinematic, cSt @ 100°C 14.5

- Viscosity Index 105