MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

DSG Transmission Fluid

Product Description – Direct Shift Gearbox

Midlands Lubricants DSG Transmission Fluid is specially formulated, fully synthetic Dual Clutch Transmission fluid is suitable for a wide range of vehicles fitted with DSG or DCT wet transmission, including: Volkswagen, BMW, Audi, Seat and Skoda. Provides excellent friction durability, scuffing protection and fatigue resistance.

PERFORMANCE / SPECIFICATIONS

- VW TL 521 82

- BMW DCTF-1

TYPICAL PROPERTIES

- Colour Red

- Density, g.ml-3 @ 15°C 0.851

- Flash Point, COC 237°C

- Pour Point -51°C

- Viscosity Kinematic @ 40°C 36 cSt