MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

LDS Fluid

Product Description – Hydractive 3 Suspension

A orange synthetic blend hydraulic fluid specifically for citroen cars equipped with *HYDRActive3*.

FEATURES / BENEFITS

High oxidation and thermal stability Excellent fluidity at sub-zero temperatures Very low pour point

PERFORMANCE / SPECIFICATIONS

For Citroen specific *HYDRActive 3* systems PSA S71 2710

TYPICAL PROPERTIES

- Colour Orange

- Density, g.ml-3 @ 15°C 0.851

- Flash Point, COC, 170°C

- Pour Point -59°C

- Viscosity Kinematic @ 40°C 19 cSt