MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Power Steering Fluid - PSF

Product Description

Midlands Lubricants A high performance multi-application fluid meeting General Motors 6137- M Dexron II and Allison C3 specifications, and is also suitable for Ford transmissions with a red filler cap. The high viscosity index and low pour point makes this product ideal for use in hydraulic systems, power steering and torque convertors.

FEATURES / BENEFITS

- Good friction control

- High oxidation and thermal stability

- Consistent gear change performance

- Excellent fluidity at sub-zero temperatures Smooth power transmission in all working conditions

- Multi-applications: transmissions, torque convertors, power steering, and general hydraulic systems

PERFORMANCE / SPECIFICATIONS

- GM Dexron II D and GM 6137-M

- Allison C4

- Caterpillar TO-2

- Hydraulic Pump Systems: Voith, Sperry-Vickers, Sunstrand and Denison

TYPICAL PROPERTIES

- Density, g.ml-3 @ 15°C 0.869

- Flash Point, COC 210°C

- Pour Point -36°C

- Viscosity Kinematic @ 40°C 42.5 cSt

- Kinematic @ 100°C 8.3 cSt

- Viscosity Index 163