MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

SAE 30 – 4 Stroke Engine Oil

Product Description

Midlands Lubricants Four stroke engine oil is a high quality mono-grade engine oil formulated from solvent refined paraffinic base oils and high performance additives for use in heavy duty diesel engines and some petrol engines operating at high ambient temperatures.

FEATURES / BENEFITS

- Good Deposit Control Good Anti-Sludge and Varnish Resistance

- Excellent Anti-Wear and Corrosion Protection

- Oxidation Stability Dispersant/Detergent Properties

- Resistance to high sulphur fuels

- High Viscosity Index promotes High Oil Pressure

PERFORMANCE / SPECIFICATIONS

- API: SF/CD

- MIL-L-2104C

TYPICAL PROPERTIES

- Total Base Number, (TBN) 10.6 mgKOH.g-1

- Density, g.cm-3 @ 15°C 0.895

- Flash Point, COC 240°C

- Pour Point -18°C Sulphated Ash 1.17%

- Viscosity Kinematic, 40°C 105 cSt

- Kinematic, 100°C 11.6 cSt

- Viscosity Index 98