MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

15W/40 SS

API SL/CF Synthetic Engine Oil

Product Description

Midlands Lubricants 15W/40 SS is a specially formulated semi-synthetic engine oil meeting stringent European performance specifications for naturally aspirated petrol engines working under normal and arduous conditions.

Performance Specifications:

15W/40 SS meets or exceeds the performance requirements of:

API: SL/CF

ACEA: A3, B3, B4

VW: 500.00, 505.00

MB: 227.5, 229.1

Features/Benefits:

Excellent High and Low Temperature Performance

High Temperature Protection against Ring Sticking

High Levels of Engine Cleanliness

Ensured Oil Performance and Reduced Consumption.

Improved Fuel Efficiency

Long-Lasting Dispersant and Anti-Wear Performance

Good Corrosion Protection

Low Emissions

Typical Properties:

Total Base Number (TBN) 10 mgKOH/g

Specific Gravity, 15°C 0.884 g/cm3

Flash Point, COC 235 °C

Viscosity

Kinematic, 40°C 112 cSt

Kinematic, 100°C 15.0 cSt

Viscosity Index 157

Pour Point -30°C