MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Mid Mould 7

Mould Release Agent Oil

Mid Mould 7 is a general purpose mould release agent and is based on a blend of low viscosity oils. It is suitable for use on but not limited to wood, steel, and Aluminium stuttering and moulds.

Mid Mould 7 has been formulated using highly refined mineral oils together with additives to give excellent release characteristics together with an enhanced surface finish.

Mid Mould 7 is an excellent mould release agent that can be used as a wipe, sponge or spray.  Our mould release agent coating can be used to prevent surface bonding on concrete mould forms as well as wood and various other materials.

Application & Benefits

 Release agent for moulding of concrete forms

 Used on a wide variety of shuttering

 Wood Shuttering / Moulds

 Steel Shuttering / Moulds

 Aluminium Shuttering / Moulds

 Combines excellent lubricity and release agent

 Contains release additives

 High flash point

 Formulated for use on a variety of material moulds

 Light colour

 Provides an excellent surface finish

|  Easy separation from the mould |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Mid Mould 7 |  |  |  |  |  |  |  |
| Characteristics | Typical Data |  | Characteristics |  | Typical Data |  |  |
| Appearance | Amber |  | Viscosity at 40°C |  | 7 cst |  |  |
| Flash Point | 140°C |  | Specific Gravity (@20°C) |  | 0.85 |  |  |
| Ester | No |  | Biodegradable |  | No |  |  |

Mid Mould 7 Directions for use

- 3 year shelf life from manufacture.

- Designed to be used as supplied and is safe to use on most surfaces.

- Store in a cool dry place between –5°C and 30°C, material should always be stored indoors and protected from extremes of temperature.

- For guidance on handling and disposal please refer to the material safety data sheet