MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Mid Form Vanishing Oil

Synthetic Vanishing Oil ALHD.

Mid Form Vanishing Oil is a modern high quality, medium performance synthetic vanishing oil designed to give significant enhancements in tool-life, operator comfort, and surface finish. Suitable for high speed applications of up to 400 cycles/minute. The product is designed to give high performance on Aluminium and non-ferrous metals and leave zero residue.

Mid Form Vanishing Oil is a special product which is a rapidly evaporating product with low odour. This high performance product that provides good tool-life, excellent surface finish and leaves a drier residue.

Mid Form Vanishing Oil is suitable for blanking, forming, punching, and pressing of ferrous and non-ferrous metals, giving superior surface finish and tool-life

Application & Benefits

 Low odour

 Fast drying

 Multi metal compatible

 Non staining

|  Zero residue Mid Form Vanishing Oil |  |  |  |
| --- | --- | --- | --- |
| Characteristics | Typical Data | Characteristics | Typical Data |
| Appearance | Pale Liquid | Viscosity (@40oC) | 2 cst |
| Chlorine | Nil | Specific Gravity (@20oC) | 0.81 |
| Lubricity | Medium | EP Performance | Moderate |
| Sulphur | No | Refractometer Conversion Factor | N/A |

Mid Form Vanishing Oil is designed to be used as supplied and can be applied by brush, roller or spray.