MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Compressor Oil 100

Midlands Lubricants Compressor Oil ISO 100 is suitable for rotary vane compressors or other compressor requiring ISO 100. Compressor 100 is a mineral oil based lubricant designed to meet the requirements of highly rated compressors. It is formulated from extremely high quality base stock and incorporates the latest compressor oil additive technology to provide fantastic extreme pressure performance and high resistance to oxidisation, rusting and corrosion. Our Rotary Vane Compressor oil 100 is rated as a 2000 hour lubricant and is recommended for use with portable compressors, stationary compressors as well as rotary vane compressors including axial and reciprocating cylinders where ISO 100 is required.

Features/Benefits:

Long service life up to 2000 hours

Ashless formulation

High Viscosity Index and Excellent Extreme Pressure performance

Good Anti-Wear Performance and Protection

High Resistance to Oxidation, Rust and Corrosion for Long Life Lubrication

Performance/Specifications:

Rotary Vane Compressor Oil 100 meets a comprehensive range of performance and specification requirements including:

DIN 51506

DIN 51523 Part 2: PNEUROP Oxidisation

Typical Properties:

Density, g.cm-3 @ 15.6°C = 0.889

Flash Point, COC 225°C

Pour Point -11°C

Viscosity

Kinematic, 40°C = 100 cSt

Kinematic, 100°C = 9.8 cSt

Viscosity Index 95    - Sulphated ash <0.01

These data are typical of current production, and whilst future production will meet these specifications, some variation in typical data may occur.