MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Compressor Oil 68 SAE 20

Midlands Lubricants Compressor Oil ISO 68 SAE 20 is suitable for rotary vane compressors or other compressor requiring ISO 68. Compressor 68 SAE 20 is a mineral oil based lubricant designed to meet the lubrication requirements compressors. It is formulated with low carbon forming characteristics from extremely high quality base stock and incorporates the latest compressor oil additive technology to provide fantastic performance and high resistance to oxidisation, rusting and corrosion. Our Compressor oil 68 SAE 20 is great for use on compressors with critical high temperature discharge and is recommended for use with screw compressors, portable compressors, stationary compressors as well as rotary vane compressors where ISO 68 is required.

Features/Benefits:

Low lacquer and carbon forming ensuring cleaner system

High film strength

Minimal oil carry over

Good Anti-Wear Performance and Protection

Excellent Resistance to Oxidation, Rust and Corrosion

Performance/Specifications:

Vane Compressor Oil 68 SAE 20 meets a comprehensive range of performance and specification requirements including:

ISO 6743-3A-DAH

Seal Compatibility with Sealing materials commonly used in Air Compressors

Typical Properties:

Density, g.cm-3 @ 15.6°C = 0.880

Flash Point, COC 230°C

Pour Point -25°C

Viscosity

Kinematic, 40°C = 68 cSt

Kinematic, 100°C = 8.6 cSt

Viscosity Index 100

These data are typical of current production, and whilst future production will meet these specifications, some variation in typical data may occur.