MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Biodegradable Chainsaw Oil 100

Product Description:

Midlands Lubricants Biodegradable chainsaw oil is a vegetable oil based lubricant which is an environmentally acceptable alternative to conventional mineral oil based chainsaw fluids.

Our Biodegradable chainsaw oil is formulated from naturally occurring vegetable oil with viscosity improver and tackiness additives for anti fling. Biodegradable chainsaw oils are recommended for use in agricultural and forestry applications were special care is required to protect the environment should a catastrophic loss occur.

Features/Benefits:

Corrosion Protection, DIN 51585A A-0

CEC L-33-T-82 Biodegradability, > 90%

Incorporates a viscosity improver additive that enables a wide temperature range of service with excellent non fling and adhesion.

Multi use biodegradable chain lubricant with high viscosity for improved film strength.

Typical Properties:

Density, 15.6°C 0.950 g/cm3

Flash Point, COC 270°C

Pour Point -10°C

Biodegradability, CEC L-33-T-82 > 90%

Viscosity

Kinematic, @ 40°C = 90 cSt

Kinematic, @ 100°C = 10.5 cSt

Viscosity Index 100

Data are typical of current production, and whilst future production will meet these specifications, some batch to batch variation in typical data may occur.