MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

5w/40 Motorcycle Full Synthetic Engine Oil – T4 API SL/CF

# Product Description

Midlands Lubricants 5w/40 Full synthetic engine oil with JASO MA2 Anti-slip is specially formulated full synthetic engine oil for of high performance with ultimate protection and cleanliness. 5w/40 is a synthetic oil which exceeds the highest international specification and OEM motorcycle manufacturers requirements.

FEATURES / BENEFITS

Exceptional thermal stability helping resist oxidisation and high-temperature derogation. Optimise wet clutch performance along with maximum shear stability to help resist viscosity shear. Outstanding protection against engine wear as well as wear of transmission components. Excellent low temperature characteristics to help minimise engine wear during start up.

PERFORMANCE / SPECIFICATIONS

- API: SL/CF

- ACEA: A3, B3, B4

- JASO MA2

TYPICAL PROPERTIES

- Total Base Number (TBN) 10 mgKOH/g

- Specific Gravity, 15°C = 0.884 g/cm3

- Flash Point, COC 214 °C

- Viscosity Kinematic, 40°C = 96 cSt

- Kinematic, 100°C = 14.8 cSt

- Viscosity Index 139

- Pour Point -30°C