MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

0w/30 Full Synthetic Engine Oil A5/B5

Product Description

Fully Synthetic 0W/30 engine oil Full Synthetic A5/B5 is a high performance motor oil produced from high quality synthetic base oils that produces outstanding performance with high fuel. 0w/30 Engine Oil A5,B5 meet the latest passenger specification for Euro IV compliant engine that do not require treatment devices.

Features/Benefits:

Excellent Protection – Protects the engine against wear

Excellent deposit control

Protection against sludge formulation

Provides optimum performance for vehicles requiring A5,B5

Performance / Specifications:

Full Synthetic 0W/30 A5,B5 meets the performance requirements of the following:

API: SL/CF

ACEA: A5-B5

BMW: LL01

VW: 503.00 / 506.00

MB: 229.5

Typical Properties:

TBN, mgKOH.g-1 = 10.0

Density, g/cm3 @ 15°C = 0.860

Flash Point, COC = 210°C

Pour Point = -35°C

Viscosity

Kinematic, @ 40°C = 55 cSt

Kinematic, @ 100°C = 9.5 cSt

Viscosity Index = 157

These data are typical of current production, and whilst future production will meet these specifications, some

variation in typical data may occur.