MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

0w/30 Full Synthetic Engine Oil C3

Product Description

Fully Synthetic 0W/30 engine oil C3 is produced from high quality synthetic base oils and top-tier performance additives.

Features/Benefits:

Suitable for use in petrol and diesel engines requiring VW specified

lubricant performance

Blended to ensure fuel efficiency, reduced wear and low emissions.

Low SAPS technology delivers a high level of engine cleanliness and

protection from combustion contamination.

Provides optimum performance and engine protection at temperature

extremes and under high performance conditions.

Performance / Specifications:

FS 0W/30 meets the performance requirements of the following:

API: SN/CF

ACEA:C3-12

BMW: Longlife-04

GM: Dexos 2 (formerly GM GEOS)

MB: 229.31, 229.51

Typical Properties:

TBN, mgKOH.g-1 = 7.5

Density, g/cm3 @ 15°C = 0.856

Flash Point, COC = 220°C

Pour Point = -40°C

Viscosity

Kinematic, @ 40°C = 67 cSt

Kinematic, @ 100°C = 11.5 cSt

Viscosity Index = 167

These data are typical of current production, and whilst future production will meet these specifications, some

variation in typical data may occur.