CoolSpec Supreme VR11

Technical Data Sheet

COOLSPEC SUPREME VR11 is an ethylene glycol based engine coolant concentrate, which uses Organic Acid Inhibitor Technology and is free from nitrites, amines, phosphates, borates and silicates. BTC Classification Type 4E. Fleet trials have shown that when used at the correct concentration coolants based on Organic Acid Inhibitor Technology continues to provide effective corrosion protection for up to 250,000 km for passenger cars and 500,000km in commercial vehicles. It is recommended that the coolant is replaced when the above mileages have been reached or after 5 years which ever is the sooner. Unlike traditional coolants which employ inorganic inhibitors, COOLSPEC SUPREME VR11 has excellent hard water stability and very low inhibitor depletion rates.

Physical Properties

|  | rameter |  |  |  | Method |  |  | VR11 |  |  | STM D3306 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Specific Gravity |  |  |  | ASTM D 4052 |  |  | 1.125 |  |  | 1.110 – 1.145 |  |  |
|  | 15/15°C |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Equilibrium Reflux |  |  |  | ASTM D 1120 |  |  | 174 |  |  | 163 min |  |  |
|  | Boiling Point °C |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Freezing Point °C |  |  |  | ASTM D 1177 |  |  | -40 |  |  | -37 max |  |  |
|  | (50% Dilution by vol.) |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Freezing Point °C |  |  |  | ASTM D 1177 |  |  | -20 |  |  |  |  |  |
|  | (33% Dilution by vol.) |  |  |  |  |  |  |  |  |  |  |  |  |
|  | pH (50% vol.) |  |  |  | ASTM D |  |  | 8.0 |  |  | 7.5 – 11.0 |  |  |
|  |  |  |  |  | 1287 |  |  |  |  |  |  |  |  |
|  | Reserve Alkalinity |  |  |  | ASTM D |  |  | 7.5 |  |  | Report |  |  |
|  | 0.1N HCl |  |  |  | 1121 |  |  |  |  |  |  |  |  |
|  | Water Content |  |  |  | ASTM D 1123 |  |  | 3.0 |  |  | 5 max |  |  |
|  | Foaming | Vol. (ml) |  |  |  |  |  | 45 |  |  | 150 max |  |  |
|  |  |  |  |  | ASTM D1881 |  |  |  |  |  |  |  |  |
|  | Properties | Break |  |  |  |  |  | 2 |  |  | 5 max |  |  |
|  |  | (s) |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  | Page 1 of 4 pages |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | TDS/COOLSPEC SUPREME VR11/47182/007 Aug 2017 |  |  |  |  |  |

Corrosion Protection

ASTM D1384 Glassware Corrosion Test Results.

|  |  |  |  |  |  |  |  | Weight Loss mg/ Coupon |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Copper |  |  | Solder |  |  | Brass |  |  | Steel |  |  | Cast |  |  | Aluminium |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  | Iron |  |  |  |  |
| ASTM |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| D3306 |  | 10 |  |  | 30 |  |  | 10 |  |  | 10 |  |  | 10 |  |  | 30 |  |
| (max) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| VR11 |  | 1.0 |  |  | 0.6 |  |  | -0.7 |  |  | 1.9 |  |  | 0.1 |  |  | -0.7 |  |

ASTM D 4340 Corrosion of Aluminium under heat rejecting conditions

|  |  | Weight Loss mg/ cm²/week |  |
| --- | --- | --- | --- |
| ASTM D 3306 (max) |  | 1.0 |  |
| VR11 |  | 0.2 |  |

ASTM D2570 Simulated Service Corrosion Test

|  |  |  |  |  |  |  |  | Weight Loss mg/ Coupon |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Copper |  |  | Solder |  |  | Brass |  |  | Steel |  |  | Cast |  |  | Aluminium |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  | Iron |  |  |  |  |
| ASTM |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| D2570 |  | 20 |  |  | 60 |  |  | 20 |  |  | 20 |  |  | 20 |  |  | 60 |  |
| (max) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| VR11 |  | 2 |  |  | 3 |  |  | 2 |  |  | 2 |  |  | 1 |  |  | 5 |  |

ASTM D2809 Cavitation Corrosion Characteristics of Aluminium Pumps

|  | Visual Rating |
| --- | --- |
| ASTM D 2809 (min) | 8 |
| COOLSPEC SUPREME VR11 | 9 |

(The above figures are typical values and do not constitute a specification.  )

Page 2 of 4 pages

TDS/COOLSPEC SUPREME VR11/47182/007 Aug 2017

Freeze Protection

|  |  |  |  |  | Concentration by Volume % |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 25 |  |  | 33 |  |  | 40 |  |  | 50 |  |  | 60 |  |
| Specific Gravity |  | 1.040 |  |  | 1.055 |  |  | 1.073 |  |  | 1.086 |  |  | 1.100 |  |
| 20/4°C |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Freeze |  | -12 |  |  | -22 |  |  | -27 |  |  | -40 |  |  | -56 |  |
| Protection * °C |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| *Average of Freezing Point and Pour Point |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

Performance Standards

COOLSPEC SUPREME VR11 exceeds the requirements of most European and International Standards including:

ASTM D3306

ASTM D 4985 SAE J 1034

BS 6580 (2010) AFNOR NF R15-601 * FFV Heft R443

CUNA NC 956-16

UNE 26361 - 88 JIS K 2234 * NATO S 759

(* with the exception of reserve alkalinity)

It also meets the performance requirements of the following OEM specifications:

Chrysler MS 9176

Cummins CES 14603

Ford ESE M97B49-A, WSS-M97B44-D &ESD M97 B49-A

GM 1899 M, US 6277 M & OPEL GM QL130100

John Deere H 24 B1 & C1

Leyland Trucks LTS 22 AF 10

Mack 014GS 17004

MAN 248, 324 (SNF) & B&W D 36 5600

Mercedes MB 325.3

Renault 41-01-001 - D

VAG TL 774 D/F

VOLVO VCS

Page 3 of 4 pages

TDS/COOLSPEC SUPREME VR11/47182/007 Aug 2017

Compatibility with other coolants

COOLSPEC SUPREME VR11 is compatible with other ethylene glycol based coolants and can be safely mixed with them. As COOLSPEC SUPREME VR11 employs an inhibitor technology that is significantly different from that used in traditional coolants we recommend that prior to using COOLSPEC SUPREME VR11 in systems previously filled with traditional coolant that the cooling system is drained and flushed with clean water before filling with COOLSPEC SUPREME VR11 diluted in accordance with the vehicle manufacturers instructions to ensure optimum performance and durability. Failure to do so can significantly reduce the working life of the coolant. In the absence of a vehicle manufacturer’s advice we would recommend a 50% dilution of COOLSPEC SUPREME VR11 in good quality water.

Page 4 of 4 pages

TDS/COOLSPEC SUPREME VR11/47182/007 Aug 2017